SECTION 03051

CONCRETE COLOR ADDITIVE

NOTE ** Delete either section number and title above or that below.  If both are required, choose one number and edit the title to suit.

SECTION 04051

MASONRY COLOR ADDITIVE

NOTE ** Davis Colors concrete and masonry color additives.

NOTE **

NOTE ** This section is based on products of Davis Colors, located at:

NOTE **    7101 Muirkirk Road       3700 E. Olympic Boulevard

NOTE **    Beltsville, MD 20705     Los Angeles, CA 90023

NOTE **    Tel:  (800) 638-4444     Tel:  (800) 356-4848

NOTE **    Tel:  (301) 210-3400     Tel:  (213) 269-7311

NOTE **    Fax:  (301) 210-4967     Fax:  (213) 269-1053

NOTE **    Visit our Web site at http://www.daviscolors.com

NOTE ** Davis Colors add color to the design of concrete floors, structures, and masonry.  Integral colors are economical to use because they are mixed right in and require little additional labor.  In addition, integral colors are permanent and do not require periodic refinishing as can coatings and applied finishes.  Davis Colors are made with pure, concentrated pigments especially milled for mixing into concrete.  They are lightfast, alkali-resistant, weather resistant, and formulated to give long-lasting appeal to concrete.

NOTE **

NOTE ** SECTION 03051 - CONCRETE COLOR ADDITIVE, Copyright 1997, The Architect's Catalog, Inc.

PART 1	GENERAL

1.1	SECTION INCLUDES

NOTE ** Delete items below not required for project.  This section is written under the assumption that the basic requirements for the work are specified in at least one other section, leaving only the provisions relating to the color additive in this section.

NOTE **

NOTE ** Note, however, that an exact color match between concrete specified in different sections may not be practical because of the differences in the manufacturing and construction processes; make final color selections on the basis of mock-ups.  Colored masonry also may not match concrete for the same reason; make color selection from actual manufactured products.

A.	Requirements For Color Additive Used In:

1.	Portland cement concrete paving specified in Section 02751.

2.	Stamped pattern concrete paving specified in Section _____.

3.	Concrete unit pavers specified in Section 02780.

4.	Cast-in-place concrete specified in Section 03300.

5.	Architectural concrete specified in Sectio 03330.

6.	Exposed aggregate concrete specified in Section 03365.

7.	Precast concrete specified in Section 03400.

8.	Architectural precast concrete specified in Section 03451.

9.	Tilt-up precast concrete specified in Section 03470.

10.	Masonry specified in Section 04810.

11.	Concrete roofing tiles specified in Section 07321.

1.2	RELATED SECTIONS

NOTE ** Delete any sections below not relevant to this project; add others as required.

A.	Section 07900 - Joint Sealers: Colored sealants for joints.

1.3	REFERENCES

NOTE ** Other applicable sections should reference appropriate standards for the basic work:

NOTE **

NOTE ** For concrete:  ACI 301, ACI 318, ACI 305R, ACI 306R, ACI 304.

NOTE ** For precast concrete:  PCI MNL 116, 120, 122.

NOTE ** For paving:  ACI 316R.

NOTE ** For tilt-up:  ACI C4.

NOTE ** For masonry:  ACI 530, ACI 530.1.

NOTE **

NOTE ** For a copy of ASTM C 979, contact Davis Colors.

NOTE **

NOTE ** Other useful publications about colored concrete include:

NOTE ** ACI 303R - Cast-In-Place Architectural Concrete Work.

NOTE ** PCA PA124.H - Finishing Concrete Slabs with Color and Texture.

NOTE ** PCA SP021A - Color and Texture in Architectural Concrete.

A.	ASTM C 309 - Liquid Membrane-Forming Compounds for Curing Concrete; American Concrete Institute.

B.	ASTM C 979 - Standard Specification for Pigments for Integrally Colored Concrete.

1.4	SUBMITTALS

A.	Submit under provisions of Section 01300.

B.	Product Data:  Manufacturer's specifications and instructions for pigments and curing compounds.

NOTE ** Delete the following paragraph if colors have been pre-selected and are specified.

C.	Samples for Pigment Color Selection:  Pigment manufacturer's color chart or sample chip set; indicate pigment number and required dosage rate.

D.	Samples for Verification of Pigment Color:  Sample chips of specified colors indicating pigment numbers and required dosage rates.  Submittals are for general verification of color and may vary somewhat from concrete finished in field according to Specifications.

NOTE ** Delete the following paragraph if no special aggregate is specified.  These samples will not be useful in determining the actual color that will be produced -- only the mock-up can do that.

E.	Samples of Aggregate and Sand.

F.	Samples for Verification of Precast Concrete:  _____ samples, 2 foot by 2 foot (610 mm by 610 mm) indicating concrete color range, texture, and uniformity.

G.	Samples for Verification of Unit Pavers:  _____ samples of each style and color, taken from actual production run, in manufacturer's standard size.

H.	Samples for Selection of Concrete Masonry:  Masonry manufacturer's standard colors.

I.	Samples for Verification of Concrete Masonry Units:  Samples of each color and style, taken from actual production runs.

1.5	QUALITY ASSURANCE

NOTE ** Specify a mock-up to demonstrate that proposed materials and workmanship produce acceptable appearance and color.  Note:  Samples submitted for color selection can be used only for general color selection; actual colors in completed work will differ -- use the mock-up.  If color additive is used for more than one application it may be necessary to construct a mock-up for each, due to differences in methods that might change the result.

A.	Mock-Up:  Provide full-scale mock-up to demonstrate methods of obtaining consistent visual appearance.

1.	Coordinate mock-up requirements with mock-ups specified in other sections; same mock-up may be used for more than one purpose.

2.	Construct at least one month before start of actual work, using materials and methods to be used in actual work.

3.	Paving:  4 x 4 feet (1.2 x 1.2 m).

4.	Precast Concrete:  Construct mock-up in plant or on site.

5.	Locate mock-up on site.

6.	Retain samples of materials used in mock-up for comparison with materials used in remaining work.

7.	Accepted mock-up constitutes visual standard for work.

NOTE ** Delete one of the following two paragraphs.

8.	Mock-up may remain.

9.	Remove mock-up when no longer required for comparison with finished work.

NOTE ** Specify preconstruction conference if job is complex.

B.	Preconstruction Conference:  Conduct a review of procedures required to produce results.

1.6	DELIVERY, STORAGE AND HANDLING

A.	Pigments: Comply with manufacturer's instructions.  Deliver pigments to site or batch plant in original, unopened packaging.  Store in dry conditions.

1.7	PROJECT CONDITIONS

A.	Plant-Mixed Concrete:  Schedule delivery of concrete to provide consistent mix times from batching until discharge.

B.	Concrete Paving:  Schedule placement to minimize exposure to wind and hot sun before curing materials are applied.  Avoid placing concrete if rain, snow or frost is forecast within 24 hours.  Protect fresh concrete from moisture and freezing.

C.	Tilt-Up Concrete:  Schedule work to minimize differences in time that panels remain on casting slab in order to minimize differences in curing conditions.  When possible, apply curing compound to panels as soon as they are put into place.

PART 2	PRODUCTS

2.1	MANUFACTURERS

A.	Concrete Pigments:  Provide products manufactured by Davis Colors, 7101 Muirkirk Road, Beltsville, MD 20705. ASD. Tel: (800) 638-4444, In MD: (301) 210 3400. Fax: (301) 210-4967. or 3700 E. Olympic Boulevard, Los Angeles, CA 90023. ASD. Tel: (800) 356-4848, In CA: (213) 269-7311. Fax: (213) 269-1053.

NOTE ** Delete one of the following two paragraphs; coordinate with Division 1 requirements.

B.	Requests for substitutions will be considered in accordance with provisions of Section 01600.

C.	Substitutions:  Not permitted.

2.2	COLORS

NOTE ** Delete all but one of the following descriptions of required concrete  colors.  Use the first paragraph to specify an existing sample, either in small size located in a place the contractor can visit, or on an existing building.

NOTE **

NOTE ** Use the second paragraph to specify matching a mock-up constructed after award of contract.  Use the third paragraph if neither of the first 2 options is appropriate.

A.	Concrete Colors:  Provide cement, aggregate, and pigment as required to match ____________.

B.	Concrete Colors:  Provide cement, aggregate, and pigment as required to produce consistent colors matching approved mock-up.

C.	Concrete Colors:  Provide cement, aggregate, and pigment as required to produce consistent colors using the materials specified.

NOTE ** The colors of all the materials affect the final appearance.  Use the following sub-paragraphs to specify the colors required, for either option 2 or 3 above.  The following is an example of how to specify simple walls and floors.  If other applications are required, with different colors, copy one set of paragraphs and identify each with a different name.

D.	Exterior Walls:

NOTE ** Gray cement is standard.  White cement may be needed to produce some colors, particularly pastel colors, but is considerably more expensive than gray cement.

1.	Cement:  Gray.

NOTE ** Delete all but one of the following three paragraphs.  Selection of actual colors before bidding is the preferred method, as the color and the dosage rate can significantly affect the cost.  Typical dosage rates range from 1 to 5 percent and must not exceed 10 percent.

2.	Color Additive:  Colors as indicated on drawings.

3.	Color Additive:  Davis Colors pigment No.___ at dosage rate of ___ percent.

4.	Color Additive:  Color to be selected by Architect from Davis Colors subtle, standard, and premium color lines.

NOTE ** The following two sub-paragraphs should be include only if colors have not yet been selected.

a.	Allow for ____ different pigment colors.

b.	Allow for up to ___ percent dosage for each color.

5.	Sand:  Manufactured white sand.

NOTE ** Delete aggregate if standard concrete/masonry aggregate is acceptable.  Otherwise, define both what the aggregate is and what color it is.

6.	Aggregate:  ______________.

NOTE ** Some fabricators prefer to pour panels in two layers.  Delete the following paragraph if not acceptable.

7.	Precast Concrete:  At Contractor's option, uncolored concrete may be used for concealed portion, provided colored face layer is fully bonded to backing.

E.	Concrete Floors:

1.	Cement:  Gray.

NOTE ** Delete all but one of the following three paragraphs.  Selection of actual colors before bidding is the preferred method, as the color and the dosage rate can significantly affect the cost.  Typical dosage rates range from 1 to 5 percent and must not exceed 10 percent.

2.	Color Additive:  Colors as indicated on drawings.

3.	Color Additive:  Davis Colors pigment No. ___ at dosage rate of ___ percent.

4.	Color Additive:  Color to be selected by Architect from Davis Colors subtle, standard, and premium color lines.

NOTE ** The following two paragraphs should be included only if colors have not yet been selected.

a.	Allow for ____ different pigment colors.

b.	Allow for up to ___ percent dosage for each color.

NOTE ** Exposed aggregate finishes change color as the aggregate is exposed, because the cement paste is washed off and the color of the sand and aggregate become more visible.

5.	Sand:  Locally available natural sand.

NOTE ** Delete aggregate if standard concrete/masonry aggregate is acceptable.  Otherwise, define both what the aggregate is and what color it is.

6.	Aggregate:  ________.

NOTE ** Delete non-slip aggregate if not required for surface of floor slabs or paving.  Silicon carbide gives a sparkling appearance; aluminum oxide does not.

7.	Non-Slip Aggregate:  Black silicon carbide.

8.	Non-Slip Aggregate:  Gray aluminum oxide grains.

NOTE ** Delete all but one of the following three paragraphs.

F.	Colored Mortar:  Match _______.

G.	Colored Mortar:  Match approved mock-up.

H.	Colored Mortar:

NOTE ** Use white cement to obtain the lightest colors on the True Tone Sweet 16 color card.

1.	Cement:  White.

NOTE ** Delete all but one of the following three paragraphs.  Selection of actual colors before bidding is the preferred method, as the color and the dosage rate can significantly affect the cost.  The dosage rate ranges from 1/2 box to 4 boxes.

2.	Color Additive:  Colors as indicated on drawings.

3.	Color Additive:  Davis Colors True Tone color No. ___ at rate of ___ dose-sized 1-1/2 lb boxes per sack of cement or lime.

4.	Color Additive:  Color to be selected by Architect from Davis Colors True Tone Sweet 16 color lines.

NOTE ** The following two sub-paragraphs should be included only if colors have not yet been selected.

a.	Allow for ____ different pigment colors.

b.	Allow for up to ___ dose-sized boxes for each color.

5.	Sand:  Locally available natural sand.

NOTE ** Delete all but one of the following three paragraphs.

I.	Colored Concrete Masonry Units:  Color to be selected by Architect from Davis Color subtle, standard, and premium color lines.  Allow for ____ different colors.

J.	Colored Concrete Masonry Units:  Match ________.

K.	Colored Concrete Masonry Units:

NOTE ** Delete all but one of the following three paragraphs.  Selection of actual colors before bidding is the preferred method, as the color and the dosage rate can significantly affect the cost.  Typical dosage rates range from 1 to 5 percent and must not exceed 10 percent.

1.	Color Additive:  As indicated on drawings.

2.	Color Additive:  Davis Colors pigment No. ___ at dosage rate of ___ percent.

3.	Color Additive:  Color to be selected by Architect from Davis Colors subtle, standard, and premium color lines.

NOTE ** The following two sub-paragraphs should be included only if colors have not yet been selected.

a.	Allow for ____ different pigment colors.

b.	Allow for up to ___ percent dosage for each color.

NOTE ** White cement produces a light color unit.

4.	Cement:  Gray.

5.	Sand:  Locally available natural sand.

NOTE ** Delete aggregate if standard concrete/masonry aggregate is acceptable.  Otherwise, define both what the aggregate is and what color it is.

6.	Aggregate:  ________.

2.3	MATERIALS

NOTE ** In general, integrally colored concrete and masonry can be specified with the same cements, aggregates, reinforcing, forms, and admixtures used in high-quality uncolored concrete.  Specify here any different materials that are needed to produce the colored work required.

A.	Colored Concrete Additive:  Pure, concentrated mineral pigments especially processed for mixing into concrete and complying with ASTM C 979.

1.	Base dosage rates on weight of portland cement, fly ash, silica fume, lime and other cementitious materials but not aggregate or sand.

NOTE ** Delete the following paragraph if only site-mixed concrete or mortar are required.  Mix-Ready disintegrating bags simplify use of pigments. Toss unopened Mix-Ready bags directly into concrete mixer.  Bags travel deep into mix and disintegrate under mixing action, so there's less colored dust released into air and no empty sacks to litter job site.  Premeasured bags make it easy to add the right amount of pigment without weighing.  Additional packaging systems are also available for convenience of ready mix plant operators.

2.	Packaging: If pigments are to be added to mix at site, furnish pigments in premeasured Mix-Ready disintegrating bags to minimize job site waste.

B.	Admixtures: Do not use calcium chloride admixtures.

NOTE ** Delete one of the following two paragraphs.  Use only curing compounds specifically recommended for use with colored concrete.  Davis Colors W-1000 Clear Cure & Seal is formulated for colored concrete and exposed aggregate finishes and complies with ASTM C 309 curing compound specification.  Color Seal II, which is tinted, gives the surface a semi-transparent coat of color for a more uniform, less natural appearance.

C.	Curing Compound for Colored Concrete:  Davis Colors W-1000 Clear Cure & Seal; complying with ASTM C 309.

D.	Curing Compound for Colored Concrete:  Davis Colors Color Seal II tinted to match colored concrete; ASTM C 309.

NOTE ** Delete any of the following material specifications if the appropriate provisions are made in the other applicable sections.

NOTE **

NOTE ** Porous materials, like lumber or unfaced plywood, can absorb moisture from fresh concrete, causing uneven curing and colors.  Decorative form liners provide textured or patterned relief on the concrete surface and increase the design possibilities with colored concrete.  Leakage through joints in forms changes the water-to-cement ratio near the joint, leading to a change in color.

E.	Form Facing Material:  Smooth, non-porous surface; steel, plastic, or high-density overlaid plywood, as permitted by applicable specification; with watertight joints, sealed to prevent leakage.

NOTE ** Conventional metal form ties can rust if not properly recessed and plugged.  Colored fiberglass ties blend with concrete when ground flush to surface and do not rust.

F.	Form Ties: Fiberglass rods tinted to match concrete.

NOTE ** Use corrosion-resistant chairs and supports to prevent rust stain on face of concrete.

G.	Supports for Reinforcing Bars:  Use corrosion-resistant types at locations in contact with exposed surfaces.

NOTE ** Be sure that the applicable sections specify a form release agent that is non-staining and minimizes formation of "bug-holes" in surface of concrete.

2.4	MIXES

NOTE ** When specifying concrete mix, 4" slump is recommended.  If greater slump is required, use water-reducing or super-plasticizing admixture instead of adding water.  Low water-cement ratio promotes richer, darker concrete colors.

A.	Concrete Mix:  Mix pigments in accordance with manufacturer's instructions, until pigments are uniformly dispersed throughout mixture and disintegrating bags, if used, have disintegrated.

PART 3	EXECUTION

3.1	FORMED SURFACES

A.	See applicable sections.

NOTE ** See ACI 301 and PCA Color and Texture in Architectural Concrete for information about formed finishes.

NOTE **

NOTE ** The following finishes will have the more uniform color than as-cast finishes:

NOTE ** Textured form liner finish.

NOTE ** Exposed aggregate, scrubbed finish.

NOTE ** Exposed aggregate, blast finish.

NOTE ** Exposed aggregate, tooled finish.

NOTE **

NOTE ** Removing forms when concrete is at various ages can result in color variations.

B.	Stripping:  Leave forms in place as long as practical.  Remove forms when concrete has reached a consistent age to maintain uniformity of curing conditions throughout Project.

C.	Sandblasted Finish:  Allow concrete to cure to sufficient strength that it will not be damaged by blasting but not less than seven days.

3.2	FLOORS AND PAVING

NOTE ** The following are just two of many possible finishes with integrally colored concrete.  Finishing Concrete Slabs with Color and Texture published by Portland Cement Association is a useful guide and includes photographs of these and other finishes.

A.	See applicable sections for additional requirements.

NOTE ** Brooming provides an attractive, slip-resistant surface.  Applying broomed finish to floated concrete saves the extra step of troweling and can produce a more uniformly colored surface.

B.	Broomed Finish:  Do not dampen brooms.

NOTE ** The smooth, dense surface produced by troweling may not provide adequate slip resistance outdoors or in wet areas.  Over-troweling or starting troweling late may produce discolored burns or dark spots.

C.	Trowel Finish:  Do not over-trowel or start troweling late.

NOTE ** Delete the following paragraph if not required.  Edit the rate of application as required.

D.	Non-Slip Aggregate Finish:  Uniformly spread aggregate over surface at 1/4 lb/sq ft (1 kg/sq m) and lightly trowel to embed in surface.

3.3	PATCHING CONCRETE

A.	Fill holes and defects in concrete surface within 48 hours of form removal.

B.	Use the same patching materials and techniques that were approved on mock-up.

C.	Make patches with a stiff mortar made with materials from the same sources as the concrete.  Adjust mortar mix proportions so dry patch matches dry adjacent concrete.  Add white cement to mortar mix if necessary to lighten it.

D.	Exposed Aggregate Finish:  Add aggregate to mortar mix so patches will have the same texture and appearance as adjacent concrete.

3.4	CURING CONCRETE

A.	Maintain concrete between 65 and 85 F (18 to 29 C) degrees during curing.

NOTE ** Curing with an approved curing compound is recommended whenever possible.  Curing with steam or water can change the water-cement ratio of the concrete, causing a change in the concrete's color.  Curing with plastic sheets or non-appproved compounds can also discolor concrete.

B.	Cure concrete using curing compound; apply curing compound in accordance with manufacturer's instructions.

NOTE ** If other techniques are required due to precast manufacturing processes, verify that appearance of resulting concrete is acceptable.  Note that sand blasting or other exposed aggregate finishes are less affected by curing method.

1.	Precast Concrete:  If use of curing compound is not practical, use curing techniques which have been shown to adequately cure concrete and which produce acceptable color and appearance.

3.5	CLEANING MASONRY

A.	Use the least aggressive cleaning techniques possible.  Comply with recommendations of masonry and pigment manufacturers.

B.	Do not use hydrochloric acid on colored masonry or mortar.

3.6	TOLERANCES

NOTE ** As with any natural material, some variation in appearance is a normal design feature of concrete and mortar, whether colored or not.  Note that concrete and mortar lighten as they cure; allow up to 28 days for process to occur.

A.	Minor variations in appearance of colored concrete/mortar, which are similar to natural variations in color and appearance of unpigmented concrete/mortar, are acceptable.

END OF SECTION